## Slide 1: Hop-Decorate Tutorial High-throughput Atomistic Workflow for Chemically Complex Materials
Peter Hatton
MST-8
In collaboration with the Thrust 1 team of 20220063DR: Accelerated Dynamics Across Computational and Physical Scales
https://gitlab.lanl.gov/peter_hatton/hopdecorate

## Slide 2
Agenda
Motivation and context for the code development.
Main functionality (State Space Mapping and Redecoration)
Parallelization strategies
Worked examples.

## Slide 3
Agenda
Motivation and context for the code development.
Main functionality (State Space Mapping and Redecoration)
Parallelization strategies
Worked examples.

## Slide 4
Accelerated Dynamics Across Computational and Physical Scales Thrust 1: Point defect transport in MPEAs.
Cluster dynamics models of damage evolution
Automated
Loop
Given
Interatomic potential
Alloy composition
Defect

## Slide 5
State Space in ‘Simple’ Materials
In a ‘Simple’ material – vacancy defect transport is fully characterized by
1 unique state and 1 unique transition.
Notes: IN SOMETHING LIKE PURE NI, WE FIND 1 VAC POSITION AND 1 BARRIER AND WE’RE DONE.
Can just do MSD and get the D tensor
IN SOMETHJING LIKE NI20CR WE HAVE TO FIND ~ X VACANCY POSTIIONS AND ~Y BARRIERS…
Current methodologies are not sufficient – it’s a sampling issue…
The trajectory will be the sum of many such hops over a multitude of environments
We can’t a priori enumerate all hops… what do we do???

## Slide 6
State Space in ‘Simple’ Materials
In a ‘Simple’ material – vacancy defect transport is fully characterized by
1 unique state and 1 unique transition.
State Space
Notes: IN SOMETHING LIKE PURE NI, WE FIND 1 VAC POSITION AND 1 BARRIER AND WE’RE DONE.
Can just do MSD and get the D tensor
IN SOMETHJING LIKE NI20CR WE HAVE TO FIND ~ X VACANCY POSTIIONS AND ~Y BARRIERS…
Current methodologies are not sufficient – it’s a sampling issue…
The trajectory will be the sum of many such hops over a multitude of environments
We can’t a priori enumerate all hops… what do we do???

## Slide 7
State Space in ‘Simple’ Materials
In a ‘Simple’ material – vacancy defect transport is fully characterized by
1 unique state and 1 unique transition.
State Space
Notes: IN SOMETHING LIKE PURE NI, WE FIND 1 VAC POSITION AND 1 BARRIER AND WE’RE DONE.
Can just do MSD and get the D tensor
IN SOMETHJING LIKE NI20CR WE HAVE TO FIND ~ X VACANCY POSTIIONS AND ~Y BARRIERS…
Current methodologies are not sufficient – it’s a sampling issue…
The trajectory will be the sum of many such hops over a multitude of environments
We can’t a priori enumerate all hops… what do we do???

## Slide 8
A vacancy in a concentrated alloy encounters many different chemical environments
Swinburne, Thomas D. Computational Materials Science 193 (2021): 110256.
The characterization of transport will be the sum of many such hops over a multitude of environments
State Space in Chemically Complex Materials
Notes: IN SOMETHING LIKE PURE NI, WE FIND 1 VAC POSITION AND 1 BARRIER AND WE’RE DONE.
Can just do MSD and get the D tensor
IN SOMETHJING LIKE NI20CR WE HAVE TO FIND ~ X VACANCY POSTIIONS AND ~Y BARRIERS…
Current methodologies are not sufficient – it’s a sampling issue…
We can’t a priori enumerate all hops… what do we do???

## Slide 9
A vacancy in a concentrated alloy encounters many different chemical environments
State Space
Swinburne, Thomas D. Computational Materials Science 193 (2021): 110256.
The characterization of transport will be the sum of many such hops over a multitude of environments
State Space in Chemically Complex Materials
Notes: IN SOMETHING LIKE PURE NI, WE FIND 1 VAC POSITION AND 1 BARRIER AND WE’RE DONE.
Can just do MSD and get the D tensor
IN SOMETHJING LIKE NI20CR WE HAVE TO FIND ~ X VACANCY POSTIIONS AND ~Y BARRIERS…
Current methodologies are not sufficient – it’s a sampling issue…
We can’t a priori enumerate all hops… what do we do???

## Slide 10
The Closed Loop

## Slide 11
The Closed Loop
Pathways and barriers for defect migration
Atomistics

## Slide 12
State Space in Chemically Complex Materials
Hop Dec Approach

## Slide 13
State Space in Chemically Complex Materials
Hop Dec Approach
Composition of Interest

## Slide 14
State Space in Chemically Complex Materials
Hop Dec Approach
Composition of Interest
Simple Analogous Structure (“Ansatz”)

## Slide 15
State Space in Chemically Complex Materials
Hop Dec Approach
State Space
Composition of Interest
Simple Analogous Structure (“Ansatz”)
Map State Space of Simple Structure

## Slide 16
State Space in Chemically Complex Materials
Hop Dec Approach
State Space
Composition of Interest
Simple Analogous Structure (“Ansatz”)
Map State Space of Simple Structure
Encode the barrier variation in the transition

## Slide 17
Agenda
Motivation and context for the code development.
Main functionality (State Space Mapping and Redecoration)
Parallelization strategies
Worked examples.

## Slide 18
Nudged Elastic Band like you’ve NEBer seen it before…
Current NEB implementation in LAMMPS is insufficient to implement high-throughput barrier calculations.
Connection
Transition
initialState (State)
finalState (State)
dE
Transition
initialState (State)
finalState (State)
Forward Barrier
dE
Forward Barrier
Output

## Slide 19
Nudged Elastic Band like you’ve NEBer seen it before…
Current NEB implementation in LAMMPS is insufficient to implement high-throughput barrier calculations.
Connection
Transition
initialState (State)
finalState (State)
dE
Transition
initialState (State)
finalState (State)
Forward Barrier
dE
Forward Barrier
Output
Initial State
Final State
Step 1: Initial NEB calculated between user-defined Initial and Final State.

## Slide 20
Nudged Elastic Band like you’ve NEBer seen it before…
Current NEB implementation in LAMMPS is insufficient to implement high-throughput barrier calculations.
Connection
Transition
initialState (State)
finalState (State)
dE
Transition
initialState (State)
finalState (State)
Forward Barrier
dE
Forward Barrier
Output
Initial State
Final State
Step 1: Initial NEB calculated between user-defined Initial and Final State.

## Slide 21
Nudged Elastic Band like you’ve NEBer seen it before…
Current NEB implementation in LAMMPS is insufficient to implement high-throughput barrier calculations.
Connection
Transition
initialState (State)
finalState (State)
dE
Transition
initialState (State)
finalState (State)
Forward Barrier
dE
Forward Barrier
Output
Initial State
Final State
Step 1: Initial NEB calculated between user-defined Initial and Final State.
Step 2: NEB Nodes minimized to search for intermediate minima.
Intermediate
State

## Slide 22
Nudged Elastic Band like you’ve NEBer seen it before…
Current NEB implementation in LAMMPS is insufficient to implement high-throughput barrier calculations.
Connection
Transition
initialState (State)
finalState (State)
dE
Transition
initialState (State)
finalState (State)
Forward Barrier
dE
Forward Barrier
Output
Initial State
Final State
Step 1: Initial NEB calculated between user-defined Initial and Final State.
Step 2: NEB Nodes minimized to search for intermediate minima.
Step 3: NEB calculated between new states in correct order.
Intermediate
State

## Slide 23
Nudged Elastic Band like you’ve NEBer seen it before…
Current NEB implementation in LAMMPS is insufficient to implement high-throughput barrier calculations.
Connection
Transition
initialState (State)
finalState (State)
dE
Transition
initialState (State)
finalState (State)
Forward Barrier
dE
Forward Barrier
Output
Initial State
Final State
Step 1: Initial NEB calculated between user-defined Initial and Final State.
Step 2: NEB Nodes minimized to search for intermediate minima.
Step 3: NEB calculated between new states in correct order.
Step 4: Go To Step 2
Intermediate
State

## Slide 24
Nudged Elastic Band like you’ve NEBer seen it before…
Current NEB implementation in LAMMPS is insufficient to implement high-throughput barrier calculations.
Connection
Transition
initialState (State)
finalState (State)
dE
Transition
initialState (State)
finalState (State)
Forward Barrier
dE
Forward Barrier
Output
Initial State
Final State
Step 1: Initial NEB calculated between user-defined Initial and Final State.
Step 2: NEB Nodes minimized to search for intermediate minima.
Step 3: NEB calculated between new states in correct order.
Step 4: Go To Step 2
Step 5: If no intermediate minima detected. End.
Intermediate
State

## Slide 25
Nudged Elastic Band like you’ve NEBer seen it before…
Current NEB implementation in LAMMPS is insufficient to implement high-throughput barrier calculations.
Connection
Transition
initialState (State)
finalState (State)
dE
Transition
initialState (State)
finalState (State)
Forward Barrier
dE
Forward Barrier
Output
Initial State
Final State
Intermediate
State
Connection: Between any two states.
Transition: Single saddle point between states – contains several useful Attributes
A Connection can contain many Transitions.
Connection object returned to the user.

## Slide 26
Nudged Elastic Band like you’ve NEBer seen it before…
Connection
Transition
initialState (State)
finalState (State)
dE
Transition
initialState (State)
finalState (State)
Forward Barrier
dE
Forward Barrier
Output
Connection: Between any two states.
Transition: Single saddle point between states – contains several useful Attributes.
A Connection can contain many Transitions.
Connection object returned to the user.
# read HopDec parameters
params = getParams()
# read atomic configurations from file.
initialState = readStateLAMMPSData('DV1.dat')
finalState = readStateLAMMPSData('DV2.dat’)
# run the NEB method and save as a Connection object
connection = neb.main(initialState, finalState, params)
for i in range(len(connection.transitions)):
  print(f'Transition {i+1}')
  print(f"{connection.transitions[i].forwardBarrier = } eV")
  print(f"{connection.transitions[i].reverseBarrier = } eV")
  print(f"{connection.transitions[i].KRA = } eV")
  print(f"{connection.transitions[i].dE = } eV \n")

## Slide 27
State Space Mapping (NEB + MD)
Notes: Canonical label and centrosymmetry
Model contains info.

## Slide 28
State Space Mapping (NEB + MD)
HASH = 1
State Space Model
Notes: Canonical label and centrosymmetry
Model contains info.

## Slide 29
State Space Mapping (NEB + MD)
HASH = 1
State Space Model
Notes: Canonical label and centrosymmetry
Model contains info.

## Slide 30
State Space Mapping (NEB + MD)
HASH = 2
HASH = 1
State Space Model
Notes: Canonical label and centrosymmetry
Model contains info.

## Slide 31
State Space Mapping (NEB + MD)
HASH = 2
HASH = 1
State Space Model
Transition
Notes: Canonical label and centrosymmetry
Model contains info.

## Slide 32
State Space Mapping (NEB + MD)
HASH = 2
HASH = 1
State Space Model
Transition
HASH = 1
Notes: Canonical label and centrosymmetry
Model contains info.

## Slide 33
State Space Mapping (NEB + MD)
HASH = 2
HASH = 1
State Space Model
Transition
HASH = 1
Notes: Canonical label and centrosymmetry
Model contains info.

## Slide 34
State Space Mapping (NEB + MD)
HASH = 2
HASH = 1
State Space Model
Transition
Notes: Canonical label and centrosymmetry
Model contains info.

## Slide 35
State Space Mapping (NEB + MD)
HASH = 2
HASH = 1
State Space Model
Transition
Notes: Canonical label and centrosymmetry
Model contains info.

## Slide 36
State Space Mapping (NEB + MD)
HASH = 2
HASH = 1
State Space Model
Transition
HASH = 3
Notes: Canonical label and centrosymmetry
Model contains info.

## Slide 37
State Space Mapping (NEB + MD)
HASH = 2
HASH = 1
State Space Model
Transition
HASH = 3
Transition
Notes: Canonical label and centrosymmetry
Model contains info.

## Slide 38
State Space Mapping (NEB + MD)
HASH = 2
HASH = 1
State Space Model
Transition
HASH = 3
Transition
Notes: Canonical label and centrosymmetry
Model contains info.

## Slide 39
State Space Mapping (NEB + MD)
HASH = 2
HASH = 1
State Space Model
Transition
HASH = 3
Transition
HASH = 4
Notes: Canonical label and centrosymmetry
Model contains info.

## Slide 40
State Space Mapping (NEB + MD)
HASH = 2
HASH = 1
State Space Model
Transition
HASH = 3
Transition
HASH = 4
Transition
Notes: Canonical label and centrosymmetry
Model contains info.

## Slide 41
State Space Mapping (NEB + MD)
HASH = 2
HASH = 1
State Space Model
Transition
HASH = 3
Transition
HASH = 4
Transition
Notes: Canonical label and centrosymmetry
Model contains info.

## Slide 42
State Space Mapping (NEB + MD)
HASH = 2
HASH = 1
State Space Model
Transition
HASH = 3
Transition
HASH = 4
Transition
Transition
Notes: Canonical label and centrosymmetry
Model contains info.

## Slide 43
State Space Mapping (NEB + MD)
HASH = 2
HASH = 1
State Space Model
Transition
HASH = 3
Transition
HASH = 4
Transition
Transition
Notes: Canonical label and centrosymmetry
Model contains info.

## Slide 44
State Space Mapping (NEB + MD)
HASH = 2
HASH = 1
Transition
Notes: Canonical label and centrosymmetry
Model contains info.

## Slide 45
State Space Mapping (NEB + MD)
HASH = 2
HASH = 1
Transition
User-defined Concentration of species
,
,
,……..,
Notes: Canonical label and centrosymmetry
Model contains info.

## Slide 46
State Space Mapping (NEB + MD)
HASH = 2
HASH = 1
Transition
User-defined Concentration of species
,
,
,……..,
Energy Barrier
0.0
0.5
Concentration of ‘Green’
Notes: Canonical label and centrosymmetry
Model contains info.

## Slide 47
HASH = 2
HASH = 1
State Space Model
Transition
HASH = 3
Transition
HASH = 4
Transition
Transition
Hop-Decorate Main Functionality

## Slide 48
Redecoration
Initial State
Final State
Given an initial Transition:
And a user-provided concentration of species and number of decorations we can redecorate the transition and calculate the energy barrier.
,
,
,……..,

## Slide 49
Redecoration
Initial State
Final State
Given an initial Transition:
And a user-provided concentration of species and number of decorations we can redecorate the transition and calculate the energy barrier.
,
,
,……..,
Concentration of ‘Green’
Energy Barrier
0.0
0.5

## Slide 50
Redecoration
Redecoration
…
Connection
Redecorate.connections
‘params.nDecorations’ – many connections
Connection
Connection
Connection
Transition
Transition
Transition
Transition
Transition
initialState (State)
List of transitions:
Connection.transitions
finalState (State)
KRA
dE
initialState (State)
finalState (State)
KRA
dE
initialState (State)
finalState (State)
KRA
dE
transition.initialState
transition.finalState
transition.KRA
transition.dE
# read HopDec parameters
params = getParams()
# load structures from file
initialState = readStateLAMMPSData('DV1.dat')
finalState = readStateLAMMPSData('DV2.dat’)
Redecoration = Redecorate.main(initialState, finalState, params)

## Slide 51
Agenda
Motivation and context for the code development.
Main functionality (NEB, Discovery and Redecoration)
Parallelization strategies
Worked examples.

## Slide 52
Strong Focus on Parallelization
Given, say, 100 MPI ranks we have two parallelization strategies:
Strategy 1: MD State discovery
Strategy 2: Redecoration
Hash = 1: ranks 0 - 24
Hash = 2: ranks 25 - 49
Hash = 3: ranks 50 - 74
Hash = 4: ranks 75 - 99
Redecoration NEB Campaign (10,000 Decorations)
,
,
,……..,
Rank = 0: Decorations 0 - 99
Rank = 1: Decorations 100 - 199
Rank = 2: Decorations 200 - 299
… and so on …
‘gather’ used to collect data onto rank 0 when redecorations are finished.

## Slide 53
Agenda
Motivation and context for the code development.
Main functionality (NEB, Discovery and Redecoration)
Parallelization strategies
Worked examples.

## Slide 54
https://gitlab.lanl.gov/peter_hatton/hopdecorate